- ****-* (Don’t edit this line.)

- Critical buckling load of a three-layer sandwich Timoshenko beam resting on a Kerr elastic foundation

  - 1 Abolfazl Akramibostanabad, 2,*Mehdi Mohammadimehr

    - 1MSc Student, 2Professor

1,2 Department of Solid Mechanics, Faculty of Mechanical Engineering, University of Kashan, Kashan, 87317-53153, Iran.

      - *Corresponding Author: mmohammadimehr@kashanu.ac.ir

          - This study presents analytically the buckling behavior of a thin three-layered carbon/epoxy–nomex honeycomb–carbon/epoxy sandwich Timoshenko beam resting on Kerr elastic foundation. The beam is modeled using Timoshenko beam theory to account for transverse shear deformation, which may be significant due to the relatively low shear stiffness of the Nomex honeycomb core. The displacement field is defined in terms of the transverse displacement of the mid-plane and the rotation of the cross-section, from which the axial and transverse shear strains are obtained. The total potential energy is formulated by considering the strain energy of the sandwich beam, the elastic potential energy of the Kerr foundation, and the potential associated with the applied axial compressive load. The equilibrium equations are obtained by applying the principle of minimum potential energy. The constitutive relations are then used to determine the stress resultants and the extensional, bending–extension coupling, bending, and transverse shear stiffness coefficients. Since the three layers configuration of the beam structure is symmetric. The three parameters of the Kerr foundation are retained in the governing equations to examine their effects on the buckling load. For simply supported boundary conditions, the Navier method is used to obtain the modal equations for the transverse displacement and cross-sectional rotation. The resulting equations form a coupled algebraic system, and the critical axial load for each mode is obtained from the corresponding characteristic equation. The lowest critical value among the admissible modes is taken as the buckling load of the sandwich beam.

Buckling behavior; Sandwich Timoshenko beam; Kerr elastic foundation; Principle of minimum potential energy.

Introduction

Sandwich structures, with thin stiff face sheets and a light compliant core, combine a high bending stiffness with a low weight. They are used in aircraft floors, fairings, control surfaces and rotor blades, in launch-vehicle and UAV structures, and also used in naval and armored defense platforms. Glass-fiber skins also keep radomes transparent to radar, whereas carbon-fiber skins give the highest stiffness.

The main limit of these thin-walled members under compression is buckling. Because honeycomb cores like Nomex [1] have a low shear modulus, transverse shear deformation lowers the buckling load, an effect ignored by Euler–Bernoulli theory but included in Timoshenko theory [2]. In service, panels are also bonded to frames, foam or compliant substructures, which behave as an elastic foundation. The Kerr model [3] describes it with two springs and a shear layer.

A closed-form critical load allows fast screening of materials and dimensions in early design, before costly finite-element or test campaigns. This paper derives it for a symmetric sandwich Timoshenko beam on a Kerr foundation and studies the effect of slenderness, resin and fiber type.

Theoretical Formulation

Kinematics and constitutive relations

Consider a beam of length L, width b and thickness h, with two identical face sheets of thickness 0.2h and a core of thickness hc = 0.6h. Timoshenko theory assumes u(x,z) = u0(x) + zψ(x) and w(x,z) = w0(x), where u0 and w0 are the mid-plane displacements and ψ is the cross-section rotation. The strains are

εx=u0'+zψ',   γxz=ψ+w0'	(1)

Each layer obeys σx = Q11εx and τxz = Q55γxz. Integrating through the thickness gives the extensional, coupling, bending and shear stiffnesses A11, B11, D11 and S = κsA55, where κs is the shear correction factor. The layup is symmetric, hence B11 = 0.

Equilibrium and Navier solution

The total potential energy sums the strain energy, the foundation potential and the potential of the axial load N0. The lower spring kl, upper spring ku and shear layer kg of the Kerr foundation reduce to Kw = klku/(kl + ku) and Ks = kgku/(kg + ku). Minimum potential energy gives the equilibrium equations

N'= 0M'-Q= 0Q'-N0-Ksw0″-Kww0= 0	(2)

Materials and Numerical Procedure

The face sheets are unidirectional glass and carbon fiber/epoxy laminates with fiber volume fraction Vf = 0.6 and four epoxy resins (Table 1). Glass fibers have Ef1 = 72.4 GPa, Gf12 = 38.03 GPa, νf = 0.229; carbon fibers 225 GPa, 30.20 GPa, 0.20; Ef2 = 15.64 GPa for both. E1 and ν12 follow the rule of mixtures, E1 = VfEf1 + VmEm, and E2 and G12 the Halpin–Tsai relation [4], P = Pm(1 + ξηVf)/(1 − ηVf),

with η = (Pf/Pm − 1)/(Pf/Pm + ξ), where P is E2 (ξ = 2) or G12 (ξ = 1), and G13 = G12. The Nomex core has E1 = 44.5 MPa, E2 = 4.4 MPa, G13 = 14.6 MPa and ν12 = 0.2606. The beam has h = 5 mm, b = h/4 and κs = 0.5. The foundation is defined by kl = ku = 10−5A11/L and kg = 10−6A11L. The slenderness study uses isotropic face sheets (E = 1.44 GPa, ν = 0.3) and modes n = 1–20.

Results and Discussion

Critical load versus mode number for different slenderness ratios L/h.

Fig. 1 plots Ncr(n) against the mode number for slenderness ratios from 5 to 200. Every curve rises with n, so the first mode is critical in all cases. The buckling load falls from 1.52×105 at L/h = 5 to 1.33×102 at L/h = 200. Short beams flatten near S = 5.76×105, the shear-stiffness bound in Eq. (3), so for stubby members core shear limits the load. The Kerr terms change the load by under 0.5% up to L/h = 100.

Effect of the resin on the critical load of glass-fiber face sheets, L/h = 20.

Fig. 2 compares the four resins for glass-fiber skins at L/h = 20. All curves nearly coincide at the first mode, which is governed by D11 and therefore by the fiber, and they separate at higher modes, where the load approaches the shear-controlled value and the resin matters. LR620 gives the highest load, since its larger modulus raises G12 and hence S, whereas EPR 1080 is the lowest (Table 1). The first-mode spread is only about 4%, so the resin can be chosen for processing or environmental resistance.

Matrix, effective face-sheet moduli (GPa) and critical load

| Face sheet | Em | E1 | G12 | Ncr (105) |
| --- | --- | --- | --- | --- |
| Glass / EPR 1080 | 2.73 | 44.53 | 3.73 | 3.314 |
| Glass / LR620 | 4.16 | 45.10 | 5.54 | 3.457 |
| Glass / Araldite LY 556 | 3.40 | 44.80 | 4.46 | 3.389 |
| Glass / Prime 27LV | 3.30 | 44.76 | 4.34 | 3.378 |
| Carbon / LR620 | 4.16 | 136.66 | 5.35 | 9.172 |

Glass versus carbon fibers with LR620 resin, L/h = 20.

Fig. 3 shows that carbon skins triple D11 and raise the buckling load from 3.46×105 to 9.17×105, a factor of 2.65 that is below 3 because of shear flexibility. At high modes the curves converge and cross near n = 17, since carbon/LR620 has a slightly lower G12 and thus lower S. Higher modes are thus controlled by shear stiffness and the critical first mode by the fiber modulus.

Conclusion

A closed-form buckling load was derived for a symmetric sandwich Timoshenko beam on a Kerr foundation. The first mode was critical in all cases, the load followed Euler scaling for slender beams and was bounded by the shear stiffness for short ones, and carbon/LR620 face sheets gave the highest load. The formula suits fast preliminary sizing of aerospace and defense sandwich panels.

References

- Ardebili, A. et al., Enhancing Strength of Nomex Sandwich Structures through the Utilization of Nano Clay Dispersed Epoxy Resin: A Study in Aerospace Applications

- Mohammadjavad Jafari, Mehdi Mohammadimehr,. Forced vibration control of Timoshenko’s micro sandwich beam with CNT/GPL/CNR reinforced composites integrated by piezoelectric on Kerr’s elastic foundation using MCST

- Sajadian, S.A., Mohammadimehr, M. and Irani Rahaghi, M., Vibration Response of a Sandwich Higher-Order Micro Beam Based on Shear and Normal Deformation Theory on Kerr Elastic Foundation with Thickness Stretching Effect

- Halpin, J.C. and Tsai, S.W., AFML-TR-67-423, 1969.